Tender Specifications AVK Surface box H-4055V MD-GG Air Valve [80/30-101]

1. Range

4055V / height adjustable 400-535 mm / PA+

2. Product description

General

The surface box shall be for installation in tarmac roads to provide access to underground air valves.

Basic design

The surface box design shall correspond with AVK surface box H-4055V MD-GG Air Valve series 80 type 30 variant 101 (STV 80/30-101) or equivalent.

Product shall be a heat resistant, synthetic, self-adjusting surface box with a cast iron GJL-200 lid attached to the housing by a stainless steel A2-70 bolt and locking clip.

Housing shall consist of two parts made out of heat resistant PA+ material with a fixed bottom part and a floating type height adjustable top part.

Features

Surface box shall have a max. total weight of 14 Kg.

Housing shall be 100% corrosion-free.

Housing and lid shall be designed to ensure easy opening at all times

Surface box housing and lid shall have a heat resistance of at least 250 °C.

Surface box shall meet D400 load bearing capacity, tested by applying flat load on top surface.

Bottom part shall be equipped with vertical ribs for optimal fixation in road.

Surface box assembly shall have an EPDM O-ring for measuring correct height prior to actual installation (or back-filling).

Surface box shall have a height range of 400-535 mm.

Floating top part shall follow road settlement ensuring perfect alignment at all times.

Surface box lid shall have multiple holes for releasing and admitting of air (max. 340m3/h / 160m3/h)

3. Standards and approvals

Surface box design shall be derived from DVGW DIN 4055.

Surface box shall be tested according to DVGW VP310-2 requirements.

4. Sustainability

Surface box shall have a carbon footprint of max. 24 Kg. Carbon footprint (CO2 emission) shall be calculated by using Lifecycle Assessment method according to ISO 14040-44. 
Housing to be made of 100% first grind recycled thermoplastic material.

Housing and lid to be 100% recyclable after end of life.

Surface box shall contain no heavy metals or any other contamination