Tender Specifications AVK Surface Box MP LD-KU [80/22-025]

1. Range

Surface Box MP / fixed height 157 mm / PA+

2. Product description

General

The surface box shall be for installation in roads, sidewalks or green zones to provide access to underground valves in water or gas lines.

Basic design

The surface box design shall correspond with AVK Surface Box MP LD-KU series 80 type 22 variant 025 (STV 80/22-025) or equivalent.

Product shall be a heat resistant, synthetic surface box with a thermoplastic lid attached to the housing by a galvanized steel cable.

Housing shall consist of one part made out of heat resistant PA+ material.

Features

Surface box shall have a max. total weight of 1 Kg.

Housing shall be 100% corrosion-free.

Housing and lid shall be designed to ensure easy opening at all times

Surface box housing and lid shall have a heat resistance of at least 250 °C.

Surface box shall be equipped with click system to ensure lid will stay in place

Surface box housing accepts and centralises down pipes Ø 75 mm up to 118 mm directly in surface box by means of internal ribs.

Surface box shall meet B125 load bearing capacity, tested by applying flat load on top surface.

Lid shall be made out of PP GF40 material.

Crossbar in lid shall be made out of A2 material.

3. Sustainability

Surface box shall have a carbon footprint of max. 2 Kg. Carbon footprint (CO2 emission) shall be calculated by using Lifecycle Assessment method according to ISO 14040-44. 
Housing to be made of 100% first grind recycled thermoplastic material.

Housing and lid to be 100% recyclable after end of life.

Surface box shall contain no heavy metals or any other contamination.